AN131

REPAINTING A SONETT

I recently completed a complete repainting of my '72 Sonett, and since I learned a lot in the process, I thought a summary might be useful to the Club members.

Do to the expansion mismatch between the paint and fiberglass a Sonett's finish will become crazed over time. External stresses and dents and dings add to this problem, as does one or more extra coats of paint. To achieve the original quality finish, it is usually necessary to remove the paint, particularly when the car has two or more coats. 80 or 120 grit paper should be used, if a hand sanding or also when using an orbital air-power sander. Extreme care must be used with any power sander to avoid removing the fiberglass below the paint. If the car has extra coats of paint, water-washable automotive paint remover may be used, but the original finish appears to be polyurethane based and will not come off with paint remover. All hand sanding should be done with a sanding block; without a sanding block, small dips and waves which are invisible when the finish is dull will appear with the finish coat.

After paint removal, fiberglass repairs should be made. Any cracks should be ground out and the fiberglass rebuilt (use mat, not cloth). Sand to achieve the correct lines with a block or body file with 50 or 60 grit paper. If imperfect, use a standard body filler to smooth contours, again with a block. Major repairs should be built from the inside out. The beauty of fiberglass is that with are any part of the car can be rebuilt.

With paint removed and repairs made, primer can be applies. It is not necessary to prime a smooth surface; with a heavy bodied primer such as Dupont 110S (thinned 1:1) even 50 grit scratches are filled. Prime and the sand with 180 watersand paper using some mild soap in the water. Remove all but a very thin layer of primer, then reprime and sand with 120 grit paper, The surface is now ready for painting.

A choice between enamel and acrylic lacquer must be made. For the amateur, lacquer allows more room for error; enamel is faster, less steps, but mistakes are difficult to repair and a truly dust-free painting room is required. I chose to use lacquer for these reasons. A base coat of color is applied and sanded smooth with 320 grit water sandpaper. Paint should be thinned about 1.5:1 with an average thinner like 3608S Dupont for the base coat. The goal is always to leave the thinnest possible layer of paint. If any dips or gouges have shown up, they should be sanded to fiberglass, filled with filler, primed and basecoated. Do not try to fill dips with primer or paint.

The final coats should be applied with a slow drying thinner to allow a smooth finish. For a final touch a few coats of clear lacquer can be applied after sanding with 600 grit paper. When dry, the paint can be buffed with a wool bonnet and polishing compound.

This kind of a paint job is not easy, but with some work and care you can achieve a finish as good or better than new.