AN190

SONETT ROCKER PANEL RUST REPAIR

1). Remove rust-thin areas.

2). Remove jack supports-grind, roll, tear off.

3). Remove "undercoating," loose dirt, scale, etc. from interior.

4). Paint interior, especially corners and crevices with Rustoleum Red.

5). Paint interior (over Rustoleum) with enamel .

6). Match repair section, drill 3 or 4 locating holes through floor and through outer rocker.

7). Trim ends of repair section to match existing.

8). Braze new jack pads to repair section (bend pads to conforming shape first).

9). Clean up, epoxy coat, locate repair section on car (using 3 or 4 jacks, wood blocks, large rubber mallet, prayer, etc.).

10). Insert 3 or 4 pop rivets, and rivet in place from center toward ends, alternating between floor pan and outer rocker--check and fit.

11). Drill and place rivets, fitting repair panel as you go (complete this fitting-riveting before epoxy sets).

12). Coat rivets with epoxy & paint.  Epoxy any places where repair panel does not fit.

13). Paint repair panel.

1