AN289

CAUSE OF BALANCE SHAFT BEARING FAILURE

I read with interest Peter McLaughlin's article on V-4 balance shaft bearings (Jan 87 NINES). I have been into a number of these engines and it rare that I find one much over 100K that doesn't have some signs of balance shaft bearing failure. It is always the same kind: pieces of the soft layer of the bearing flake off and work their way out, falling into the pan. This kind of failure is also seen occasionally on connecting rod bearings and its cause is fatigue.

Modern shell bearings are made up in layers. Beginning with a steel support shell, the bearing is built up with one or more layers of various softer metals: cooper, tin, lead, aluminum, babbit or other alloy...whatever the engineer calls for. This layered approach is supposed to deliver greater load carrying strength, better particle absorption and a graded transition from soft to hard materials, and it allows the engineer to tailor the bearing for its particular duty.

Unfortunately, despite the improvements achieved by this definitely superior to thick layer or poured bearings for high stress applications, one does eventually get separation of the layers. the interface that usually seems to fail is between the steel and all the rest. Thus, when material does slough off, the piece which disappears is several thousands thick. A bearing's load carrying capacity is proportional to its load area, and when a piece sloughs off the area is reduced, increasing the load on the remaining surface. This encourages the failure to process at an increasing rate.

As long as there is some material all around the bearing, the fit will feel okay in the manual test Mr. Laughlins describes. However, I have seen extreme causes where a thin band of "babbit" will physically support the shaft all around, but a large area has disappeared elsewhere, leaving gross oil clearance which will reduce oil pressure throughout the system. Naturally, such a bearing is not far from complete failure, but will show no symptoms of noise or loose feeling.

Any time a material is subjected to pressure, it will deflect. Even the hardest steels will yield to pressure, if only a tiny amount. If you deflect a piece of stuff over and over in the same way, eventually the material will begin to change somehow. Usually its internal structure will begin to come apart and if carried far enough, structural failure will result, sometimes in a grand way. In the case of multi-layer bearings the bond between one layer and its neighbor will begin to fail.

Now why is this such a problem with balance shaft bearings?

AN289

Consider that the balance shaft is designed to throw back into the block forces which are opposed to those the engine otherwise creates, to yields a net reduction in apparent vibration. I haven't tried to run a V-4 without a balance shaft so I don;t know how vibrational a critter it actually is, but Ford, in their wisdom, deemed it would be unacceptable without the balance shaft solution. It takes a lot of energy to shake even a small engine like the V-4. That's what the balance shaft must do, and it only has two shell bearings through which to apply its peculiar energy to the block. Added to that energy is the repulsive force of the gears on the front bearing. The pressure rolls around the bearing surface like a wave, deflecting the material as it goes, and eventually the bonds break down.

It is true that any bearing will wear away with extended use, faster with too little oil pressure or with dirty oil. But these bearings are, for practical purposes, no farther from the oil pump than the mains and are closer that the rods. All the balance shaft bearing failures I have seen, however, have been from fatigue. I want to stress this because there are many components in a vehicle ( or any other mechanism) for which fatigue controls useful life. It is important to keep it in mind because, as we work on our cars (or others) we tend to call a component OK if it has ne visible signs of wearing away.

Another example: the, usual cause of ball or roller bearing failure is fatigue. As the rolling elements roll over the races that support them, under load, all surfaces deflect slightly. Again, the materials are carefully specified for resistance to these effects, but eventually they can take it no more and little flakes break off, leaving pits in the surfaces which reduce load carrying area and create points of high local loading. The hard particles go off into the lubricant.

As the particles find their way back into the paths of rolling elements, these elements must roll up and over the particles, again with dramatic point loading. In a bearing in continuous use the fatigue curve is quite steep, after a long level service life, especially if it operates in a sealed environment where particles accumulate in the lubricant (what's that you say about transmission oil changes?). A bearing can pass inspection easily until breakdown begins. The nasty question is: Where along its service life curve is the bearing I just took out of this car?

When I do transmissions I replace all the bearings, especially in the V-4 units where bearing failure is the most common cause of demise (the bearings are too small for then loads). When I do a V-4 clutch and the engine has over 100K on it, I encourage balance shaft bearing change while the engine is out. I always find flakes in the pan. I have seen a number of failures in the release arms on V-4 clutch cover assemblies if they're old (I have seen broken ones come out through the bell housing).