AN303

SONETT WINDOW REPAIR

Automobile windows can be expensive items; worse, those for rare old models can be impossible to buy.  The rear window of the Sonett II and V4 apparently fits that category and so anything that can be done to save them is of great value.  One morning I discovered a crack in the rear window of my Sonett V4.  At the suggestion of another member, I took it to a window repair franchise.  They refused to touch it for two reasons; it was the inside layer, which meant drilling overhead, and they decided the crack was too large for their repair method.

I am somewhat confused about how window-repair franchises drill, but there is a procedure used on metal cracks, particularly in aircraft, called stop-drilling.  To stop-drill, a hole is drilled at the end of a crack.  The hole acts to distribute the stress around its circumference rather than at the point at the end of the crack.  Thus the hole greatly reduces the chance of continued cracking.

To drill metal from the bottom up is no problem.  It is not difficult to drill glass from the top, but from the bottom is a problem.  There are expensive tools for drilling glass, but very adequate tools are less expensive than  a common twist drill.

It is important to understand that the procedure I am explaining is for laminated glass.  Other automobile glass is manufactured in such a way that it seldom cracks without shattering into tiny sand-like particles.

The usual way to drill glass is actually to grind through it with carborundum or diamond.  The bit is usually a tube; I used a l/8" brass tube about 2" long.  One also needs a lubricant; slowly running water is excellent.  Now running water over something you are holding above you is not easy.  If properly done, the lubricant serves two additional purposes:  cooling and carrying sharp, fresh abrasive to replace dull, old abrasive.

In order to avoid overheating I used an air drill at 15psi.  An electric drill with either electric or gear reduction could be used.  The lubricant was K-Y jelly (from any drug store) into which I had mixed coarse carborundum powder to form a thick paste.

If this idea scares you, it may just show that you are cautious.  Try drilling an old bottle or a piece of window pane first.  Of course, there is some danger in this procedure, but there is a bigger danger in letting that crack in your window get larger.

The procedure:  A dab of paster is put on the end of the bit (brass tube).  The bit is placed about l/16" beyond the end of the crack.  The drill is started slowly, while it is carefully steadied.  In less than a minute, the carborundum will be spent.  It all went well, you have a l/8" round scratch just beyond the end of the crack.  Gently wipe off the paste and apply fresh paste, either directly to the glass or the bit, put the bit in the scratch and start the drill again.  After less than a minute, again clean off the spend paste and replace it.  Repeat this procedure until you reach the center of  the glass.  It should take about an hour.  The center is the laminating piece of plastic and will behave quite differently.  If you have only one crack and you do not develop new cracks during the drilling, you are ready to clean up.  Water, Q-tips and paper towels can be used effectively.  If there are other cracks, they should be drilled in the same manner.

Once dry, the hole may be filled with plastic so that it is less apparent.  Polyester fiberglass resin is a good choice.  It should be lightly catalyzed (about 2 drops per 1/2 oz.).  A syringe will aid in getting the resin to the bottom of the holes that are overhead.  It will take a minimum of two applications to fill the holes.  A single edge razor blade can be used to scrape the excess plastic away.  Later, rouge or crocus cloth can be used to polish the plastic.

If you have problems getting the necessary items for stop-drilling glass, please let me know.  A kit could easily be made up for the purpose.