AN360

V-4 GEAR LUBE

V-4 gearboxes require a 75 weight extreme pressure (EP) type lubricant, per the owners manual. The term "75 weight is a number set by the Society of Automotive Engineers (SAE) to denote viscosity of an oil. On the motor oil viscosity chart 75 weight gear oil is roughly equivalent to a 20 weight motor oil. SAAB has a specified this light oil weight oil to facilitate easier shifting, and to prevent cavitation at low temperatures. Cavitation is the inability of an oil to flow into the void of moving gears due to extremes of viscosity or temperatures, and the results in little or no lubrication of the critical parts until friction heats the oil and causes it to flow. The hypoid nature of the gears in the V-4 gearbox require the extreme pressure additive, and the EP additives are the most interesting aspect of gear oil.

Organic sulfur phosphorus compounds (animal fat) are the EP agents added to mineral oil, along with foam and oxidation inhibitors, this is the make up of gear oil. The sulfur phosphorus compounds are the key to what is known as boundary lubrication, and is what actually comes between moving pieces of metal at their point of contact, thus preventing wear.

What actually happens is this; a fine coating of corrosion or crust is created on metals immersed in the sulfur phosphorus oil. Known as sacrificial film lubrication, ferrous sulfate film is created on iron, and copper sulfate is created on copper or brass. This corrosion is actually the EP lubricant. As the corrosion is worn away through metal to metal contact or fluid erosion, the underlying metal is exposed and more corrosion is created.

However much corrosion is created, and is it critical to the V-04 gearbox? Volkswagen and Audi have recognized this as a problem, and specified a GL-4 rated gear oil (another standard to denote an 85-90 weight gear oil without EP additives) in many of their manual gearboxes. I believe these EP additives are responsible for the pitting seen on ring and pinion gears, and that the EP additive contributes to premature wear-out of gears and bearings.

In gearboxes that seem to average less than 75,000 miles between rebuilds, and considering the expense and scarcity of the parts involved, any unnecessary wear is unwarranted in my view.

Believing synthetic oil would prevent this from occurring, I investigated and found that while the oil is a synthetic, the additives are still organic sulfur phosphorus compounds, so the problem would still exist.

The solution is the use of a gear oil that doesn't use an organic EP additive, and it is GL-4 or better rated. While there may be others, I personally know of two products that I would believe are

AN360

superior in performance as their use alone does not guarantee some corrosion. I sell Chevron products and can recommend Chevron N.L. (no lead) Gear Compound 150 and Chevron Ultra Gear 80, or 80-90. The Chevron Ultra Gear 80 is the better of the two types of oils as it is closer to the recommended 75 weight, being an 80 weight, versus the 90 weight in the Gear Compound 150.

The Timkin rating is the heaviest load a test lubricant will sustain without scoring a test block in the Timkin Bearing Company test procedures. The higher the number the better; conventional gear oils usually rate a number between 35 and 50. Ultra Gear 80 has a Timkin rating of 75, versus a 60 rating for the N.L. Gear Compound 150.

The Chevron Ultra Gear uses an inorganic borate compound as its extreme pressure additive. The boundary lubrication film thickness of this product is three to five times that of other gear oils, and does not promote corrosion. Because it is an inorganic compounded oil, the Ultra Gear oil has better high temperature stability and longer drain intervals. Gross water contamination will cause the borate to drop out and crystalize, and this could damage seals. You should keep in mind that high concentrations of water in conventional gear oils is just as damaging in terms of rust, so those of you living in the damp regions should practice caution and occasional oil analysis to keep up with water contamination.

The only hitch is that the Ultra Gear Oil 80 and 80-90 is sold in five gallon buckets through Chevron distributors. These distributors can be found in the yellow pages of the phone book under Petroleum Lubricants. Cost is about $31.00 for five gallons, or about $1.55 per quart.

From my own experience with this oil used in a slightly whiney 1962 96 three speed resulted is an easier shifting and 20-30% less noise than when I was using the 80-90 weight conventional oil. The oil also has a much better smell than the conventional sulfur phosphorus lubricant.