AN405

SONETT RESTORATION

(Bill Jacobson of Sports Car Services in Willmington, Del., spoke on repairing Sonett chassis at the 1990 National Convention in Sturbridge, Mass.)

I'd like to start by discussing rust; location of rust and how to look for rust. All Sonett's have rust. A Sonett that's been sitting on the showroom floor with no miles on it will have rust.

SAAB never undercoated the whole underside of the Sonett. The only undercoating the wheel wells, so you find undercoating in places other than the wheel wells, theirs a good chance it's there to cover pop-riveted or sheet metal-screwed patch panels which will cause many future problems.

Take a close look around the brake line in the front. That's the first place you'll see rust, but it' one of the easiest places to repair. Right behind it lies the seam where three layers of metal come together; the belly pan, the firewall, and the floor panel.That's a difficult spot to repair. Look for blistering around the seams.

SAAB, unfortunately, did not put primer on the metal when they welded it. They caulked right over the bare metal, and then they primed the chassis. When you peel the caulking out, you'll find bare metal. If the caulking wasn't sealed or if moisture gets between those seams, it really rusts. The seam running underneath the firewall and the seam going over the top of the rear axle are the most difficult to repair and the most time consuming because it's difficult to reach all sides of the box members to clean and properly repair them.

The center floor seam is another problem. The 96 tub is not the same as a sonett tub. It can be used, but you cannot use more than two sections of the grooves. SAAB used 20 gauge sheet metal on the Sonett's and 18 gauge on the 96's, so the rows are varied, making patch panels is a little difficult to fit.

A Sonett floor is the same as a 96 trunk floor; it;'s just shortened. A narrower seam sits in the middle. Cut out about four to six inches and weld the floor back together. The Sonett II truck floor is a shortened version of the 96 trunk floor with a battery box, so while you can modify 96 chassis pieces to fit a Sonett it takes a great deal of effort. It looks as if it would be the same, but it's not exactly.

Proper chassis restoration takes approximately 100 hours of labor. If you can find somebody to do it cheaply, that's not bad, but if you have it done at the normal shop rate of about $40-45 an hour, then proper bottom panels repairs can amount to a lot of money.

AN405

Cut the rockers open. They're treated with paraffin wax only. Unfortunately, when it gets hot, the wax runs to the bottom and the sides are completely;y unprotected. Pull the carpets up on each side and cut long holes about two inches wide. Put on a heavy shirt and some rubber gloves, and clean out all that stuff along side of the seat, up by your feet and behind the rocker. Do the same with the caulking in center of the seats where the cars have no primer. The caulk is right on the bare metal. Strip the caulking away, primer, and recaulk the car.

Some of the best materials for doing this work are the two part zinc chromate primers that Duponts and other manufacture. Dupont's

numbers are 825 and 825S. It's a catalyzed paint.

Primer may be difficult to buy. Many body shops supply places will not sell it to the public due to hazardous fumes, so you may need to purchase it directly from a body shop. Wear a respirator when using the primer because it is quite nasty and you may feel nauseated when you get done. The next day you might even be sick. It's not good for you, but it's great for the car.

After priming, find a black silicone paint and paint the chassis. Silicone rubber for caulking is good, but because paint doesn't stick to it, the chassis must be painted first, and then caulked. That's the way to get the best results in sealing everything. Paint will stick to some of the better automotive latex base caulks, but they don't hold up as well.

Question: Does anyone make patch panels for the 96 or Sonett?

Apparently Tabco is going back into the manufacturing of panels. They were supposed to have them by the middle or late part of this year.

Question: Do they make patch panels for the bottom of the Sonett floorpan?

Yes. They are 96 panels, but they're made of 20 gauge sheet metal like in the Sonett instead of 18 like in the 96. They'll fit pretty well in either the Sonett or 96.

Prime with zinc chromate primer before you put them on. I restored cars in 1975 that have no rust and are driven every day, even in the salt. The only nice thing about the cold rolled steel is that it's what the car was made with and you won't encounter an electrolysis problem. If you use stainless steel or galvanized panels, electrolysis occurs as it would with an mixed metal.

Question: Once you restore a Sonett in this manner, would you expect it to last for a long time?

AN405

I restored a 1973. Fortunately, I caught it in 1975 before it had much rust. i raced it a couple of years in autocrosses and it's been used everyday since then. The only place I've had to repair is the area where the hydraulics went out on the brake master cylinder and ate the paint down around the brake master cylinder.

I last restored my last Sonett at $40 an hour. It took approximately 30 hours to strip the entire car, de-caulk, de-undercoat, re-caulk and re-undercoat the car. Now it's like new. It looks as good as ever, and now it has primer. I fund two or three little spots that need to be plugged, but no major holes. If you have a Sonett that you really want to last, re-caulk before, not after, you have problems.

Question: Is there a point at which you deem them unrestorable?

I consider a car unrestorable when the rear axle area needs repair. I repaired one in which I spent about 25 hours rebuilding the rear axle support member. I had to strengthen the rear axle inner support members because it's mounted at one place in the center. If it rusts under there, you can spend a great deal of time remaking old 96 parts. unfortunately, you can't buy the pieces.

If it's just slightly rusty and rust is not yet coming up the sides, it's acceptable. You can still strip the body off and repair the rear axle area.

If you have more than 1/8" of rust on the outside where it comes up inside the body, or the main support where the rear axle is, or if you have excessive rust anywhere, call the car quits.

When restoring a Sonett, do not put undercoating on the car. Undercoating is one of the worst things in the world for causing a car to rust. Put in only where the tires will throw up stones and chip the paint. The nice thing about paint, if you get a little blister, you can see it, scrap it, and touch it up. On the 1973 that i restored, i didn't even undercoat the wheel wells. I left everything completely open.

Use Imron or a good polyurthane paint with a Corlar base which is less likely to chip. Of all the available paints, Imron is probably one of the most impervious to brake fluid.