AN408

REVIEW FUEL LINE NIPPLE

If you remember, SAAB had a recall on the fuel line nipple leading into the carburetor.  The cars affected were 1967-1969 Sonett V4's.  Mine was loose in 1981 & I repaired it with Loctite 404 quick set per SAAB's instructions.  Early this spring while trouble shooting a problem I noticed that the fuel line (rubber) was slightly damp downstream from the clamp (towards the carburetor).  Much to my amazement the brass fitting was leaking again ever so slightly.  Pliers were necessary to remove the brass fitting as I couldn't pull it out with my fingers.

Loctite 404 is still difficult to locate through a Loctite distributor.  Fortunately the distributor took the time in the maze of cross reference charts that Loctite has to help me find a more readily available solution.  Loctite 640 is the next generation of sealants above the 404.  Loctite 640 has an operating temperature from -65 degrees F to +400 degrees F.  Loctite 404 is only good to +175 degrees F.  I suspect that the under the hood temperature plus time infringes near or above the 175 degrees mark.

While inspecting the carburetor (disassembled) I found the riser feed tube in the bottom of the float.  Similar in construction to the fuel line nipple (brass press fit into a die case body).  You can visually inspect for this if you look down into the carburetor (very carefully) to determine if the riser pipe is feeding the main throat.