AN425

PROLONGING THE USEFUL LIFE OF A CAR BATTERY

Very few car batteries are replaced because they stop working, in almost every case the battery is replaced because it doesn't work well enough any more.  What is not generally realized is that something can be done at this stage which may well prolong the useful life of the battery - quite often by many years, and that the same treatment carried out earlier in the battery's life may well have stopped the symptoms from occurring in the first place.

The reason for a battery failing to work properly any more is due to the chemical processes which take place within each cell when the battery is not fully charged.  Even the slightest of discharged conditions allows both plates to react slowly with the sulphuric acid electrolyte to form lead ions.  It is these lead ions which cause problems, they combine with sulfate ions in sulfuric acid to form highly insoluble lead sulfate.  When this coats the plates of the battery, it fails to deliver enough power to be of use.  The battery may well be thoroughly serviceable in every other way - only the "sulfating" stops the battery delivering enough power to start the car.

The sulfating can effectively be removed, or prevented, by adding to each cell a chemical called tetrasodium ethylenedianimetetraacetate (often abbreviated to tetrasodium EDTA).  This chemical forms co-ordination compounds with many metal ions, including the lead ions formed in the discharge cycle of a battery.  The compound formed by lead ions and the EDTA ion is not particularly stable in the acid medium of a  battery, but when it breaks down again any lead sulfate regenerated tends to drop to the bottom of the cell where it lays harmlessly since it doesn't conduct electricity.  Any regenerated EDTA ions are free to continue their work.

As can be seen from above, treating a battery with tetrasodium EDTA is likely to be most effective when the battery, for one reason or another, spends periods when it is not fully charged, and so contains too many lead ions.  This is likely to occur if the car is used for just short trips, is infrequently used, or has at any time suffered from an inefficient generator/alternator.  Treating with the chemical can also help keep an original battery in use, and can help in bringing back into use a stored battery.

To treat  a battery with tetrasodium EDTA you simply take a fully heaped tablespoon full of the powder, divide it up and add to each cell.  This assumed an average size of battery but the exact amount is in no way critical.  What you should then do is to use the car normally for a few days, or agitate the battery frequently for a few days, and then give it a thorough charge to build up on the cleaned plate areas.  On the assumption that sulfating has been

AN425

affecting the performance of your battery, an increased performance will be noted from here on.

Over the past few years, many thousands of European car enthusiasts have used tetrasodium EDTA with great success on their batteries.  You may wish to do the same by purchasing some of the chemical and giving it a try.  If you have problems and cannot find any tetrasodium EDTA in your locality, I can provide you with enough to treat a battery for $5.00, which includes quick dispatch by air mail.  I can readily accept personal checks made out in US dollars or cash.  My address is : K. L. Martin, 19 Brookmead, Meppershall, Shefford, Bedfordshire, S617 5SA, Great Britain.