AN 450

SONETT III HOOD - BODY PLUGS

Two of the points of attachment of the Sonett III hood are located on each sode of the body just behind the wheel wells at the bottom of the hood. A bolt goes from the inside of the wheel well and screws into a threaded fitting which is an integral part of the fiberglass body. (These are the screws marked "2" on page 820-2 of the Sonett supplement.) A common problem is to have the bolt rust and seize up in the threaded fitting. When this happens, the fitting generally tears loose inside its mounting hole and will turn as the bolt is turned.

1

Figure 1 shows the fitting which is contained in the body. It is made of a round "T-shaped" rubber plug which has a threaded metal insert. Th eplug is attached to the hood with the larger part of the rubber plug encased within the fiberglass of the hood. I bought two of these from a SAAB dealer a year ago and paid about $2.00 apiece, but it took a while to get them. The plugs are marked "WELLNUT D-1420" and are probably available from the appropiate supply house.

If you order these from SAAB, you should be aware of the following problem. The threaded inserts are made of a non-ferrous material which appears to be brass. The plug from SAAB come complete with a bolt which screws into the plug. This bolt, however, is not brass, but rather is a steel bolt which has been anodized or plated with a brass colord protective finish. This will cause problems. If the plating is scrathed or otherwise broken, the steel-bolt/brass-threaded interface causes a galvanic reaction which will corrode the bolt very quickly, causing it to seize up. Because of the location in the wheel well, it is very difficult to keep the bolt and threads clean. If you remove the hood, you are very likely to get a bit of dirt or grit in the threads. When you reattach the hood, the dirt may scratch the bolt plating. The result is instant cooroaion thge next time that it rains.

The solution to thisproblem is very simple. Replace the steel bolt with a brass bolt from your friendly neighborhood hardware store. The bolt is a standard 1/4-20 by 1" hex head bolt.

If your plugs are already loose, they can be replaced. Usually the rubber plug can be extracted from its hole without too mauch trouble. In fact, the problem is ussually that the plug has already been pulled out. It is very difficult, if not impossible, to get the large end of a new plug into the hole. Fortunatly, this is not neccessary. Just glue the new plug in backwards, i.e., with the

AN 450

large end towards the center of the car. Scott Prentice says he glued replacement plugs into his car with Crazy Glue and it worked fine. If the new plug is very loose fit in the hole in the

fiberglass, crazy glue may not work. Try silicaon bathtub caulk. It should stick well to both the rubber plug and fiberglass and fill up the gaps to give a tight fit.